MAGNAFLUX DPI  PENETRANTS – RED DYE

BULK PACKS

Penetrants

Spotcheck SKL-SP2 is a solvent removable (or post emulsifiable) red colour contrast penetrant. SKL-SP1 exhibits outstanding penetrating characteristics which provide for maximum reliability in locating surface-open flaws and discontinuities.It can be used over the entire spectrum of industrial applications, where a visible penetrant inspection system meets the requirements for surface-open flaw detection.Typical applications include castings,forgings, leak testing, welds and general metal work. SKL-SP1 has also been successfully used on non-porous ceramics and similar materials. However it is not recommended for the inspection of plastic materials, as it 
may stain, soften or even dissolve the base material under test.
Product Code F15.0220-Pack Size 4 x 5 Litre

Spotcheck SKL-WP2 is a general purpose water washable red colour contrast penetrant. SKL-WP exhibits outstanding penetrating characteristics which provides for maximum reliability in locating surface-open flaws and discontinuities. SKL-WP is formulated to give excellent controlled washability over a wide temperature range and variable dwell times It can be used over the entire spectrum of industrial applications, where a visiblepenetrant inspection system meets the requirements for surface-open flaw detection. Typical applications include castings, forgings, leak testing, welds and general metal work. SKL-WP has also been successfully used on non-porous ceramics and similar materials.However it is not recommended for the inspection of plastic materials, as it may stain, soften or even dissolve the base material under test.
Product Code F15.0121-Pack Size 4 x 5 Litre
Product Code F15.0122-Pack Size 25 Litre

Developers

SKD-S2 Developer is a ready to use suspension of white developing particles in a fast drying solvent. SKD-S2 produces an opaque white coating, which provides an excellent contrasting background for SPOTCHECK OR ZYGLO penetrant indications. SKD-S2 is specially formulated to be low in sulphur and halogens and contains no chlorinated hydrocarbons. SKD-S2 non aqueous developer provides maximum sensitivity through its solvent action on the penetrant at the defect site. SKD-S2 is compatible with and approved for use with all MAGNAFLUX Spotcheck and Zyglo penetrants.
Product Code F15.0123-Pack Size 4 x 5 Litre

Removers

SKC-S cleaner / remover is a clear colourless flammable solvent used as a general pre-cleaner and penetrant remover. SKC-S is ideal for situations where chlorinated solvents are undesirable or prohibited.Its unique composition allows use on a wide range of substrates to remove oils, greases and other contaminants.
Product Code F15.0124-Pack Size 4 x 5 Litre
Product Code F15.0125-Pack Size 25 Litre