MAGNAFLUX DPI  PENETRANTS

AEROSOL CANS 400ml

Penetrants

Spotcheck SKL-SP2 is a solvent removable (or post emulsifiable) red colour contrast penetrant. SKL-SP1 exhibits outstanding penetrating characteristics which provide for maximum reliability in locating surface-open flaws and discontinuities.It can be used over the entire spectrum of industrial applications, where a visible penetrant inspection system meets the requirements for surface-open flaw detection.Typical applications include castings, forgings, leak testing, welds and general metal work. SKL-SP1 has also been successfully used on non-porous ceramics and similar materials. However it is not recommended for the inspection of plastic materials, as it may stain, soften or even dissolve the base material under test.
Product Code F15.0120

Spotcheck SKL-WP2 is a general purpose water washable red colour contrast penetrant. SKL-WP exhibits outstanding penetrating characteristics which provides for maximum reliability in locating surface-open flaws and 
discontinuities. SKL-WP is formulated to give excellent controlled washability over a wide temperature range and variable dwell times It can be used over the entire spectrum of industrial applications, where a visible penetrant inspection system meets the requirements for surface-open flaw detection. Typical applications include castings, forgings, leak testing, welds and general metal work. SKL-WP has also been successfully used on non-porous ceramics and similar materials.However it is not recommended for the inspection of plastic materials, as it may stain, soften or even dissolve the base material under test.
Product Code F15.0121

ZL-60C is a general purpose water washable fluorescent penetrants, used for a wide range of low to medium sensitivity applications. They are typically used on castings, forgings, rough and machined surfaces to find cracks,
seams, laps, laminations and porosity.
Product Code F15.0130

ZL-27A is a general purpose water washable fluorescent penetrants, used for a wide range of low to medium sensitivity applications. They are typically used on castings, forgings, rough and machined surfaces to find cracks,seams, laps, laminations and porosity.
Product Code F15.0131

ZP-9F is a ready to use suspension of white developing particles in a fast drying solvent. ZP-9F produces a light white coating, which provides an excellent contrasting background for SPOTCHECK OR ZYGLO penetrant indications. ZP-9F is specially formulated to be low in sulphur and halogens and contains no chlorinated hydrocarbons. ZP-9F non aqueous developer provides maximum sensitivity through its solvent action on thepenetrant at the defect site. ZP-9F is compatible with and approved for use with all MAGNAFLUX Spotcheck and Zyglo penetrants.
Product Code F15.0132

Developers

SKD-S2 is a ready to use suspension of white developing particles in a fast drying solvent. SKD-S2 produces an opaque white coating, which provides an excellent contrasting background for SPOTCHECK OR ZYGLOpenetrant indications. SKD-S2 is specially formulated to be low in sulphur and halogens and contains no chlorinated hydrocarbons. SKD-S2 non aqueous developer provides maximum sensitivity through its solvent action on the penetrant at the defect site. SKD-S2 is compatible with and approved for use with all MAGNAFLUX Spotcheck and Zyglo penetrants.
Product Code F15.0122

Removers

SKC-S cleaner / remover is a clear colourless flammable solvent used as a general pre-cleaner and penetrant remover. SKC-S is ideal for situations where chlorinated solvents are undesirable or prohibited.Its unique composition allows use on a wide range of substrates to remove oils, greases and other contaminants.
Product Code F15.0123