MAGNAFLUX   MPI

AEROSOL CANS -400 ml

7HF is an oil based ready to use red ink for wet method magnetic particle testing. The ink is used in conjunction with suitable magnetising equipment to locate fine surface and slightly subsurface discontinuities in ferrous materials.Typical defects found include shrink cracks, welding defects, grinding cracks, quenching cracks and fatigue cracks. 7HF gives clear Black indications when viewed in daylight.
Product Code F05.0120

14HF is an oil based ready to use fluorescent ink for wet method magnetic particle testing. The ink is used in conjunction with suitable magnetising equipment and UV(A) source to locate fine surface and slightly subsurface discontinuities in ferrous materials. Typical defects found include shrink cracks, welding defects, grinding cracks, quencing cracks and fatigue cracks.14HF gives clear fluorescent green indications when viewed in a darkened area under UV(A) of peak wavelength 365nm.
Product Code F05.0121

410HF is an oil based ready to use fluorescent ink for wet method magnetic particle testing. The ink is used in conjunction with suitable magnetising equipment and UV(A) source to locate medium surface and slightly subsurface discontinuities in ferrous materials.Typical defects found include shrink cracks, welding defects, grinding cracks, quencing cracks and fatigue cracks. 410HF gives enhanced fluorescent green indications when viewed in a darkened area under UV(A) of peak wavelength 365nm.
Product Code F05.0122

WCP-2 is a ready to use, rapid drying white contrast paint used to provide a white background to enhance visible magnetic particle indications. WCP-2 is specially formulated to produce a thin dry film giving a high opacity semi-matt finish. It is low in sulphur and halogens and contains no chlorinated hydrocarbons.
Product Code F05.0123