MAGNAFLUX  ZYGLO  DPI PENETRANTS

BULK PACKAGING

Penetrants

Zyglo ZL-15B, is a general purpose water washable fluorescent penetrant, used for a wide range of low to medium sensitivity applications. They are typically used on castings, forgings, rough and machined surfaces to find cracks, seams, laps, laminations and porosity. It exhibits outstanding penetrating characteristics which provides for maximum reliability in locating surface-open flaws and discontinuities and are safe to use on most engineering and aerospace alloys including aluminium, steel, nickel and titanium. The penetrant has been formulated to give excellent controlled washability over a wide temperature range and variable dwell times and will produce stable fluorescent indications under normal drying conditions. The penetrant fluoresce's a bright green-yellow when exposed to ultraviolet radiation (UV-A) peak wavelength of 365 nm.
Sensitivity Level 1/2. AMS2644 approved
Product Code F15.0241- Pack Size 25 litre
Product Code F15.0242- Pack Size 200 litre

Zyglo ZL-19,  is a general purpose water washable fluorescent penetrant, used for a wide range of low to medium sensitivity applications. They are typically used on castings, forgings, rough and machined surfaces to find cracks, seams, laps, laminations and porosity. It exhibits outstanding penetrating characteristics which provides for maximum reliability in locating surface-open flaws and discontinuities and are safe to use on most engineering and aerospace alloys including aluminium, steel, nickel and titanium. The penetrant has been formulated to give excellent controlled washability over a wide temperature range and variable dwell times and will produce stable fluorescent indications under normal drying conditions. The penetrant fluoresce's a bright green-yellow when exposed to ultraviolet radiation (UV-A) peak wavelength of 365 nm.
Sensitivity Level 1. AMS2644 approved
Product Code F15.0243- Pack Size 25 litre
Product Code F15.0244- Pack Size 200 litre

Zyglo ZL-60C is a general purpose water washable fluorescent penetrant, used for a wide range of low to medium sensitivity applications. They are typically used on castings, forgings, rough and machined surfaces to find cracks, seams, laps, laminations and porosity. It exhibits outstanding penetrating characteristics which provides for maximum reliability in locating surface-open flaws and discontinuities and are safe to use on most engineering and aerospace alloys including aluminium, steel, nickel and titanium. The penetrant has been formulated to give excellent controlled washability over a wide temperature range and variable dwell times and will produce stable fluorescent indications under normal drying conditions. The penetrant fluoresce's a bright green-yellow when exposed to ultraviolet radiation (UV-A) peak wavelength of 365 nm.
Sensitivity Level 2. AMS2644 approved
Product Code F15.0245- Pack Size 25 litre
Product Code F15.0246- Pack Size 200 litre

Zyglo ZL-60D, is a general purpose water washable fluorescent penetrant, used for a wide range of medium to high sensitivity applications. It is typically used on castings, forgings and machined surfaces to find cracks, seams, laps, laminations and porosity.It exhibits outstanding penetrating characteristics which provides for maximum reliability in locating surface-open flaws and discontinuities and are safe to use on most engineering and aerospace alloys including aluminium, steel, nickel and titanium. The penetrant has been formulated to give excellent controlled washability over a wide temperature range and variable dwell times and will produce stable fluorescent indications under normal drying conditions. The penetrant fluoresce's a bright green-yellow when exposed to ultraviolet radiation (UV-A) peak wavelength of 365 nm.
Sensitivity Level 2. AMS2644 approved
Product Code F15.0247- Pack Size 25 litre
Product Code F15.0248- Pack Size 200 litre

Zyglo ZL-67, is a general purpose water washable fluorescent penetrant, used for a wide range of medium to high sensitivity applications. It is typically used on castings, forgings and machined surfaces to 
find cracks, seams, laps, laminations and porosity.It exhibits outstanding penetrating characteristics which provides for maximum reliability in locating surface-open flaws and discontinuities and are safe to use on most engineering and aerospace alloys including aluminium, steel, nickel and titanium. The penetrant has been formulated to give excellent controlled washability over a wide temperature range and variable dwell times and will produce stable fluorescent indications under normal drying conditions. The penetrant fluoresce's a bright green-yellow when exposed to ultraviolet radiation (UV-A) peak wavelength of 365 nm.
Sensitivity Level 3. AMS2644 approved
Product Code F15.0251- Pack Size 25 litre
Product Code F15.0252- Pack Size 200 litre

Zyglo ZL-56 is a general purpose water washable fluorescent penetrant, used for a wide range of medium to high sensitivity applications. It is typically used on castings, forgings and machined surfaces to 
find cracks, seams, laps, laminations and porosity.It exhibits outstanding penetrating characteristics which provides for maximum reliability in locating surface-open flaws and discontinuities and are safe to use on most engineering and aerospace alloys including aluminium, steel, nickel and titanium. The penetrant has been formulated to give excellent controlled washability over a wide temperature range and variable dwell times and will produce stable fluorescent indications under normal drying conditions. The penetrant fluoresce's a bright green-yellow when exposed to ultraviolet radiation (UV-A) peak wavelength of 365 nm.
Sensitivity Level 4. AMS2644 approved
Product Code F15.0253- Pack Size 25 litre

Zyglo ZL-2C, is a general purpose post emulsifiable fluorescent penetrant, used for a wide range of medium to high sensitivity applications.It is typically used on castings, turbine components, welds, 
forgings, rough and machined surfaces to find cracks, seams, laps, laminations and porosity. It exhibits outstanding penetrating and indication stability characteristics which provides for maximum reliability in locating surface-open flaws and discontinuities It is safe to use on most engineering and aerospace alloys including aluminium, steel, nickel and titanium. This post emulsifiable (post removable) penetrant is formulated to be immiscible with water, this property guards against over-removal from defects by over washing and allows the penetrant to separate readily from water, making effluent clean up easier. ZL-2C. is used in conjunction with a hydrophilic remover or lipophilic emulsifier to render them washable with water. The penetrant fluoresce's a bright green-yellow when exposed to ultraviolet radiation (UV-A) peak wavelength of 365 nm.
Sensitivity Level 2. AMS2644 approved
Product Code F15.0260- Pack Size 25 litre
Product Code F15.0261- Pack Size 200 litre

Zyglo  ZL-27A is a general purpose post emulsifiable fluorescent penetrant, used for a wide range of medium to high sensitivity applications.It is typically used on castings, turbine components, welds, 
forgings, rough and machined surfaces to find cracks, seams, laps, laminations and porosity. It exhibits outstanding penetrating and indication stability characteristics which provides for maximum reliability in locating surface-open flaws and discontinuities It is safe to use on most engineering and aerospace alloys including aluminium, steel, nickel and titanium. This post emulsifiable (post removable) penetrant is formulated to be immiscible with water, this property guards against over-removal from defects by over washing and allows the penetrant to separate readily from water, making effluent clean up easier. ZL-27A is used in conjunction with a hydrophilic remover or lipophilic emulsifier to render them washable with water. The penetrant fluoresce's a bright green-yellow when exposed to ultraviolet radiation (UV-A) peak wavelength of 365 nm.
Sensitivity Level 3. AMS2644 approved
Product Code F15.0262- Pack Size 25 litre
Product Code F15.0263- Pack Size 200 litre

Zyglo  ZL-37 is a general purpose post emulsifiable fluorescent penetrant, used for a wide range of medium to high sensitivity applications.It is typically used on castings, turbine components, welds, 
forgings, rough and machined surfaces to find cracks, seams, laps, laminations and porosity. It exhibits outstanding penetrating and indication stability characteristics which provides for maximum reliability in locating surface-open flaws and discontinuities It is safe to use on most engineering and aerospace alloys including aluminium, steel, nickel and titanium. This post emulsifiable (post removable) penetrant is formulated to be immiscible with water, this property guards against over-removal from defects by over washing and allows the penetrant to separate readily from water, making effluent clean up easier. ZL-37 is used in conjunction with a hydrophilic remover or lipophilic emulsifier to render them washable with water. The penetrant fluoresce's a bright green-yellow when exposed to ultraviolet radiation (UV-A) peak wavelength of 365 nm.
Sensitivity Level 4. AMS2644 approved
Product Code F15.0264- Pack Size 25 litre
Product Code F15.0265- Pack Size 200 litre

Removers

ZR-10C is a water soluble remover concentrate which is used diluted as the remover / emulsifier in post removable penetrant systems.ZR-10C is generally used in the concentration range 5% to 20% in water.
Product Code F15.0277-Pack Size 25 Litre
Product Code F15.0278-Pack Size 200 Litre

ZE-4B is a ready to use fast-acting lipophilic emulsifier designed for use with Zyglo postemulsifiable dye penetrants. ZE-4B is a red viscous liquid of high flash point and low volatility and may be used with any of the following Zyglo penetrants :
Product Code F15.0279-Pack Size 25 Litre

Developers

ZP-4B is a free flowing, white fluffy powder designed to develop fluorescent indications from all Zyglo penetrants.ZP-4B is supplied ready for use. The product forms a thin film over the surface of the component to enhance defect indications.
Product Code F15.0270-Pack Size 1Kg
Product Code F15.0271-Pack Size 5Kg

ZP-5B is a powder concentrate which is mixed with water to form a suspendable developer solution.
The unique formula of ZP-5B allows it to disperse easily in water.. The material must be continually agitated during use to ensure uniformity of mix as developer particles will settle out on standing. On drying ZP-5B forms a uniform white coating which enhances fluorescent indications formed by Zyglo penetrants. At higher concentration, ZP-5B forms an enhanced opaque white coating which provides agood contrasting background for Spotcheck indications.
Product Code F15.0272-Pack Size 5Kg

ZP-14A is a white free-flowing powder, which dissolves in water to form a clear, colourless biodegradable developer solution. ZP-14A is used as a general-purpose water-soluble developer for the enhancement of indications formed by Zyglo penetrants. ZP-14A produces a uniform white porous coating when it dries. The developer film is easily removed in post inspection cleaning by a water spray. Once the developer bath has been made up, no in use agitation is required to maintain developer uniformity. ZP-14A can be used in open tanks without ventilation as the bath is non flammable and no hazardous fumes are produced. ZP-14A baths may sometimes show a trace of fluffy sediment if the water used is hard. This sediment does not interfere with the developing or removability of the product.
For a clear solution, soft water or de-ionized water is recommended.
Product Code F15.0276-Pack Size 5Kg